**Ultrafast Exciton and Carrier Dynamics in Bulk CrSBr**

Lawson T. Lloyd1, Tommaso Pincelli1,2, Túlio de Castro1, Ferdinand Menzel3, Zdeněk Sofer4, Nathan P. Wilson3, Martin Wolf1, Laurenz Rettig1, and Ralph Ernstorfer\*,1,2

1. Fritz-Haber-Institut der Max Planck Gesellschaft, Berlin, Germany
2. Technische Universität Berlin, Berlin, Germany
3. Walter Schottky Institut, Department of Physics, School of Natural Sciences, Technische Universität München, Garching, Germany
4. Chemistry Department, University of Chemistry and Technology Prague, 16628 Prague, Czech Republic

\* Corresponding author: ernstorfer@fhi-berlin.mpg.de

**ABSTRACT**

Van der Waals (vdW) layered magnets have the potential to enable novel optoelectronic and spintronic applications. Among these, CrSBr is a direct band gap semiconductor that hosts interlayer antiferromagnetic order, a highly anisotropic, quasi-1D electronic structure, and strongly bound excitons. However, understanding how the carrier and exciton dynamics couple to the underlying spin order is currently lackng. Here, we employ time- and angle-resolved photoemission spec- troscopy to map the temperature-dependent band structure and car- rier dynamics in bulk CrSBr. Time-resolved measurements reveal a rapid band renormalization of the lower conduction band that occurs during photoexcitation, pointing towards complex many-body effects govern- ing the excited state dynamics and optical properties. These results provide important experimental observations of the low-temperature electronic band structure and shed further light on the microscopic interactions driving carrier dynamics and spin order in this vdW mag- net.

**Introduction**

[2D Magnets etc]. CrSBr is a van der Waals layered magnetic semiconductor that with a direct electronic band gap, highly anisotropic optical and electronic properties, as well as pronounced many-body exciton physics which couple to the underlying magnetic order. (*1*–*4*) [Ultrfast] Previous time-resolved studies have uncovered coherent exciton-magnon coupling persisting to the nanosecond timescale (*2*, *5*, *6*) and as well as few to sub-picosecond exciton decay dynamics in bulk and monolayer CrSBr. (*7*)

Recently, trARPES has proved an incisive technique to directly probe the energetics and momentum distribtuino of bound excitons in a variety of systems. (*8*)

Here, we employ time- and angle-resolved photoemission (trARPES) to track the photoinduced femtosecond dynamics and directly probe the excitonic signatures in bulk CrSBr (**Figure 1**).

Physics of exciton Mott transition (*9*)

**Figure 1.** (a) E = 0 eV is referenced to the valence band maximum (VBM) peak at the point.

**Figure 1d** shows a two-dimensional (*kx, ky*) momentum map near the valence band maximum (VBM) at room-temperature. While the central (*kx=ky=*0) point shows suppressed intensity, the point of the second Brillouin zone is more intense (*14*, *15*).

**Results and Discussion**

To map the electronic band structure and photoinduced dynamics of bulk CrSBr, we perform time-and angle-resolved photoemission spectroscopy (trARPES) with tunable femtosecond pump pulses. Leveraging momentum microscopy, which allows for the simultaneous acquisition of both in-plane momenta (*kx, ky*) and provides a global view of the electronic band structure and electronic dynamics in a single experiment (**Figure 1**). (*10*–*12*)

~~We perform ARPES at temperatures above and below the reported bulk magnetic transition temperature (T~~~~N~~ ~~~ 132 K), at which the system hosts interlayer antiferromagnetic ordering, with intralayer ferromagnetic order persisting to higher temperatures temperature (T~~~~C~~ ~~~ 165 K).~~ (*13*) **F**

After photoexcitation (1.55 eV, ~40 fs), we observe a quasi-flat dispersion along appearing >1 eV above the valence band maximum. (**Figure 1e,f**) Such an anisotropic dispersion has been predicted theoretically and recently observed in ARPES of few-layer CrSBr in contact with metallic substrates (*16*) as well as in alkali-metal dosed bulk CrSBr. (*17*) In particular, we observe two distinct features around E ~ 1.3 eV and E ~ 2.0 eV relative to the valence band maximum. While the upper feature features more intensity near the X points in line with previous works (*16*, *17*), the lower feature is more extended along with most intensity centered around the point, indicating subtle differences between the two features (**Figure S**).

While initial experimental studies estimated the electronic band gap of bulk CrSBr to be around 1.5 eV, (*18*) recent ARPES works have suggested a possibly larger band gap of roughly 2 eV ore greater (*14*, *17*, *19*) Optical emission measurements have shown the lowest-energy exciton resonance determining the optical band gap to lie around ~1.35 eV. (*1*, *2*, *20*) Taken together, we therefore assign the two features observed in our measurements (**Figure 1**) at E ~ 1.3 eV and E ~ 2 eV to the bound exciton state and the single-particle conduction band minimum of bulk CrSBr, respectively. Notably, our assignment implies an exciton binding energy of roughly 700 meV in bulk CrSBr. This large binding energy is consistent with previous theoretical works and, to our knowledge, is the first direct measurement owing to our capability of resolving the transient electronic structure. A direct, momentum- and energetically resolved picture of the exciton, including its binding energy, in CrSBr has so far been lacking.

In recent years, momentum microscopy, by resolving both in-plane momenta simultaneously, has provided powerful insights into the orbital and real-space character of excitons in both molecular and inorganic semiconductors. (*21*) Leveraging the two-dimensional momentum maps, we retrieve the real-space exciton wavefunction of bulk CrSBr by Fourier transformation of the momentum maps (**Figure 2**). From this, we estimate the exciton Bohr radius as ~ nm and an anisotropy ratio of ~ , in reasonable agreement with previous theoretical studies. (*22*) Here, we note that we likely create excitons with excess energy and non-zero center of mass momentum given the optical excitation of 1.55 eV compared with the resonance ~1.35 eV. Our momentum- and energy-resolved observations provide direct and novel insight into the strongly bound, anisotropic excitonic states and quasi-one dimensional electronic structure.

The observation of the higher energy feature at E = 2.0 eV is striking considering the pump excitation energy of 1.55 eV is below the electronic band gap based on our assignment. **Figure 3b,c** shows the kx dispersion and the ultrafast dynamics of these two features X and CB. While there is a rapid rise of the lower energy feature, the upper feature at E = 2.0 eV exhibits a pronounced growth after photoexcitation, pointing to a dynamical process that populates this state on the ~100s fs timescale. Additionally, the dynamics of the X feature at different momenta along do not change appreciably (**Figure S**), suggesting a common origin.

To better understand the relationship between the X and CB features and the dynamics leading to the population of CB after photoexcitation, we perform further trARPES measurements with varying excitation fluence and wavelength. In particular, we pump with wavelengths close to the exciton resonance (~915 nm) as well as with wavelengths far above the band gap (400 nm). We observe change and reversal in the early-time dynamics and relative intensities of each feature such that the state CB is populated first when exciting with higher photon energies. This supports the interpretation of CB origin as the conduction band of CrSBr. Interestingly, the exciton X state, while featuring a slightly delayed rise time with respect to the CB state, is very quickly populated even with very above-gap excitation. Such a robust exciton formation could arise from the high exciton binding energy ~ 700 meV in this material and less energetically favorable dark-excitons compared to *e.g.* WSe2. (*8*)

Strong exciton-phonon coupling in CrSBr (*23*) may also lead to enhanced phonon-assisted Auger-type decay pathways. (*24*, *25*)

Time-resolved photoluminescence: 100s ps decay time as a function of temperature. [slower @ RT?, 10s ps low T] (*23*)

Defect-assoctiated excitons in CrSBr-TMD heterostructures. (*26*)

While these works therefore suggest an exciton binding energy of well over 0.5 eV based on photoluminescence measurements with exciton signatures of around ~1.35 eV,

Exciton formation has been shown to occur in tens of femtoseconds intransition metal dichalcogenides (*27*)

Excitation density and the Mott transition (*28*) in transition metal dichalcogenides. (*29*)

**Conclusions**

**Methods**

trARPES were performed on bulk CrSBr crystals were grown by … []. For ARPES measurements, bulk crystals were mechanically cleaved in ultrahigh vacuum in base pressures better than 10-10 mbar.

trARPES measurements were performed using both a momentum microscope and a hemispherical analyzer. For the momentum microscope measurements. using a high-repetition rate OPCPA (*30*) operating at ~500 kHz (*10*, *11*)

Previous investigations of two-dimensional semiconductors using ARPES have noted the presence of sample charging due to the photocurrent. In this work, we see clear effects of charging by a shifting of the energy scale at temperatures below T ~ 110 K, and thus we limit our measurements to temperatures above this limit.

**Author Contributions**

L.T.L, T.P., and T.d.C. performed ARPES experiments. F.M., N.P.W, Z.S. provided bulk crystal samples. M.W., L.R., and R.E. provided funding and infrastructure. L.T.L analyzed the data and wrote the manuscript with input from all authors.

**Acknowledgements**

This work was funded […]. L.T.L acknowledges financial support from the Alexander von Humboldt Foundation. The authors thank Florian Dirnberger and Philip Hofmann for fruitful discussions.

**References**

1. N. P. Wilson, K. Lee, J. Cenker, K. Xie, A. H. Dismukes, E. J. Telford, J. Fonseca, S. Sivakumar, C. Dean, T. Cao, X. Roy, X. Xu, X. Zhu, Interlayer electronic coupling on demand in a 2D magnetic semiconductor. *Nat. Mater.* **20**, 1657–1662 (2021).

2. Y. J. Bae, J. Wang, A. Scheie, J. Xu, D. G. Chica, G. M. Diederich, J. Cenker, M. E. Ziebel, Y. Bai, H. Ren, C. R. Dean, M. Delor, X. Xu, X. Roy, A. D. Kent, X. Zhu, Exciton-coupled coherent magnons in a 2D semiconductor. *Nature* **609**, 282–286 (2022).

3. M. E. Ziebel, M. L. Feuer, J. Cox, X. Zhu, C. R. Dean, X. Roy, CrSBr: An Air-Stable, Two-Dimensional Magnetic Semiconductor. *Nano Lett.* **24**, 4319–4329 (2024).

4. N. J. Brennan, C. A. Noble, J. Tang, M. E. Ziebel, Y. J. Bae, Important Elements of Spin-Exciton and Magnon-Exciton Coupling. *ACS Phys. Chem Au* **4**, 322–327 (2024).

5. G. M. Diederich, J. Cenker, Y. Ren, J. Fonseca, D. G. Chica, Y. J. Bae, X. Zhu, X. Roy, T. Cao, D. Xiao, X. Xu, Tunable interaction between excitons and hybridized magnons in a layered semiconductor. *Nat. Nanotechnol.*, 1–6 (2022).

6. Y. Sun, F. Meng, C. Lee, A. Soll, H. Zhang, R. Ramesh, J. Yao, Z. Sofer, J. Orenstein, Dipolar spin wave packet transport in a van der Waals antiferromagnet. *Nat. Phys.*, 1–7 (2024).

7. C. Meineke, J. Schlosser, M. Zizlsperger, M. Liebich, N. Nilforoushan, K. Mosina, S. Terres, A. Chernikov, Z. Sofer, M. A. Huber, M. Florian, M. Kira, F. Dirnberger, R. Huber, Ultrafast Exciton Dynamics in the Atomically Thin van der Waals Magnet CrSBr. *Nano Lett.* **24**, 4101–4107 (2024).

8. S. Dong, M. Puppin, T. Pincelli, S. Beaulieu, D. Christiansen, H. Hübener, C. W. Nicholson, R. P. Xian, M. Dendzik, Y. Deng, Y. W. Windsor, M. Selig, E. Malic, A. Rubio, A. Knorr, M. Wolf, L. Rettig, R. Ernstorfer, Direct measurement of key exciton properties: Energy, dynamics, and spatial distribution of the wave function. *Natural Sciences* **1**, e10010 (2021).

9. D. Guerci, M. Capone, M. Fabrizio, Exciton Mott transition revisited. *Phys. Rev. Mater.* **3**, 054605 (2019).

10. M. Puppin, Y. Deng, C. W. Nicholson, J. Feldl, N. B. M. Schröter, H. Vita, P. S. Kirchmann, C. Monney, L. Rettig, M. Wolf, R. Ernstorfer, Time- and angle-resolved photoemission spectroscopy of solids in the extreme ultraviolet at 500 kHz repetition rate. *Review of Scientific Instruments* **90**, 023104 (2019).

11. J. Maklar, S. Dong, S. Beaulieu, T. Pincelli, M. Dendzik, Y. W. Windsor, R. P. Xian, M. Wolf, R. Ernstorfer, L. Rettig, A quantitative comparison of time-of-flight momentum microscopes and hemispherical analyzers for time- and angle-resolved photoemission spectroscopy experiments. *Review of Scientific Instruments* **91**, 123112 (2020).

12. O. Karni, I. Esin, K. M. Dani, Through the Lens of a Momentum Microscope: Viewing Light‐Induced Quantum Phenomena in 2D Materials. *Advanced Materials* **35**, 2204120 (2023).

13. F. Pei, J. Yu, J. Zhou, S. Wang, D. Liu, Y. Yuan, L. Xi, F. Jin, X. Kan, C. Wang, L. Wang, W. Yan, Y. Wu, S. Wang, K. Chen, T. Ma, X. Liu, M. Yang, Q. Li, Surface-Sensitive Detection of Magnetic Phase Transition in Van Der Waals Magnet CrSBr. *Advanced Functional Materials* **n/a**, 2309335.

14. M. Bianchi, S. Acharya, F. Dirnberger, J. Klein, D. Pashov, K. Mosina, Z. Sofer, A. N. Rudenko, M. I. Katsnelson, M. van Schilfgaarde, M. Rösner, P. Hofmann, Paramagnetic Electronic Structure of CrSBr: Comparison between Ab Initio GW Theory and Angle-Resolved Photoemission Spectroscopy. *Phys. Rev. B* **107**, 235107 (2023).

15. M. Bianchi, K. Hsieh, E. J. Porat, F. Dirnberger, J. Klein, K. Mosina, Z. Sofer, A. N. Rudenko, M. I. Katsnelson, Y. P. Chen, M. Rösner, P. Hofmann, Charge transfer-induced Lifshitz transition and magnetic symmetry breaking in ultrathin CrSBr crystals. arXiv arXiv:2307.12675 [Preprint] (2023). https://doi.org/10.48550/arXiv.2307.12675.

16. M. Bianchi, K. Hsieh, E. J. Porat, F. Dirnberger, J. Klein, K. Mosina, Z. Sofer, A. N. Rudenko, M. I. Katsnelson, Y. P. Chen, M. Rösner, P. Hofmann, Charge transfer induced Lifshitz transition and magnetic symmetry breaking in ultrathin CrSBr crystals. *Phys. Rev. B* **108**, 195410 (2023).

17. S. Smolenski, M. Wen, Q. Li, E. Downey, A. Alfrey, W. Liu, A. L. N. Kondusamy, A. Bostwick, C. Jozwiak, E. Rotenberg, L. Zhao, H. Deng, B. Lv, D. Zgid, E. Gull, N. H. Jo, Large Exciton Binding Energy in the Bulk van der Waals Magnet CrSBr. arXiv arXiv:2403.13897 [Preprint] (2024). http://arxiv.org/abs/2403.13897.

18. E. J. Telford, A. H. Dismukes, K. Lee, M. Cheng, A. Wieteska, A. K. Bartholomew, Y.-S. Chen, X. Xu, A. N. Pasupathy, X. Zhu, C. R. Dean, X. Roy, Layered Antiferromagnetism Induces Large Negative Magnetoresistance in the van der Waals Semiconductor CrSBr. *Advanced Materials* **32**, 2003240 (2020).

19. M. D. Watson, S. Acharya, J. E. Nunn, L. Nagireddy, D. Pashov, M. Rösner, M. Van Schilfgaarde, N. R. Wilson, C. Cacho, Giant exchange splitting in the electronic structure of A-type 2D antiferromagnet CrSBr. *npj 2D Mater Appl* **8**, 54 (2024).

20. J. Klein, B. Pingault, M. Florian, M.-C. Heißenbüttel, A. Steinhoff, Z. Song, K. Torres, F. Dirnberger, J. B. Curtis, M. Weile, A. Penn, T. Deilmann, R. Dana, R. Bushati, J. Quan, J. Luxa, Z. Sofer, A. Alù, V. M. Menon, U. Wurstbauer, M. Rohlfing, P. Narang, M. Lončar, F. M. Ross, The Bulk van der Waals Layered Magnet CrSBr is a Quasi-1D Material. *ACS Nano* **17**, 5316–5328 (2023).

21. M. Reutzel, G. S. M. Jansen, S. Mathias, Probing excitons with time-resolved momentum microscopy. *Advances in Physics: X* **9**, 2378722 (2024).

22. T.-X. Qian, J. Zhou, T.-Y. Cai, S. Ju, Anisotropic electron-hole excitation and large linear dichroism in the two-dimensional ferromagnet CrSBr with in-plane magnetization. *Phys. Rev. Res.* **5**, 033143 (2023).

23. K. Lin, X. Sun, F. Dirnberger, Y. Li, J. Qu, P. Wen, Z. Sofer, A. Söll, S. Winnerl, M. Helm, S. Zhou, Y. Dan, S. Prucnal, Strong Exciton–Phonon Coupling as a Fingerprint of Magnetic Ordering in van der Waals Layered CrSBr. *ACS Nano* **18**, 2898–2905 (2024).

24. K. Bushick, E. Kioupakis, Phonon-Assisted Auger-Meitner Recombination in Silicon from First Principles. *Phys. Rev. Lett.* **131**, 076902 (2023).

25. B. Scharf, V. Perebeinos, Phonon-Assisted Auger Decay of Excitons in Doped Transition Metal Dichalcogenide Monolayers. arXiv arXiv:2408.00097 [Preprint] (2024). http://arxiv.org/abs/2408.00097.

26. X. Huang, Z. Song, Y. Gao, P. Gu, K. Watanabe, T. Taniguchi, S. Yang, Z. Chen, Y. Ye, Intrinsic localized excitons in MoSe$\_2$/CrSBr heterostructures. arXiv arXiv:2405.16079 [Preprint] (2024). http://arxiv.org/abs/2405.16079.

27. C. Trovatello, F. Katsch, N. J. Borys, M. Selig, K. Yao, R. Borrego-Varillas, F. Scotognella, I. Kriegel, A. Yan, A. Zettl, P. J. Schuck, A. Knorr, G. Cerullo, S. D. Conte, The ultrafast onset of exciton formation in 2D semiconductors. *Nat Commun* **11**, 5277 (2020).

28. A. Steinhoff, M. Florian, M. Rösner, G. Schönhoff, T. O. Wehling, F. Jahnke, Exciton fission in monolayer transition metal dichalcogenide semiconductors. *Nat Commun* **8**, 1166 (2017).

29. M. Dendzik, R. P. Xian, E. Perfetto, D. Sangalli, D. Kutnyakhov, S. Dong, S. Beaulieu, T. Pincelli, F. Pressacco, D. Curcio, S. Y. Agustsson, M. Heber, J. Hauer, W. Wurth, G. Brenner, Y. Acremann, P. Hofmann, M. Wolf, A. Marini, G. Stefanucci, L. Rettig, R. Ernstorfer, Observation of an Excitonic Mott Transition Through Ultrafast Core- *cum* -Conduction Photoemission Spectroscopy. *Phys. Rev. Lett.* **125**, 096401 (2020).

30. M. Puppin, Y. Deng, O. Prochnow, J. Ahrens, T. Binhammer, U. Morgner, M. Krenz, M. Wolf, R. Ernstorfer, 500 kHz OPCPA delivering tunable sub-20 fs pulses with 15 W average power based on an all-ytterbium laser. *Opt. Express* **23**, 1491 (2015).